## Slide 1
Liquid State Machine with Memristive Microwires
Jack Kendall – Rain Neuromorphics

## Slide 2
Motivation
Why hasn’t neuromorphics succeeded at the same level as deep learning?
  Lack of good neuromorphic algorithms.
  Poor scalability of fully-connected layers.

## Slide 3
But what plays the mischief with this masterly.
Sparsity is critical for scalable neuromorphic hardware
The brain uses primarily two forms of sparsity: Small-World and Scale-Free.
These forms of sparsity minimize wiring cost while maximizing network efficiency.
They allow the wiring density to scale at the same rate as the neuron density.

## Slide 4
Natural sparsity can be achieved with random memristive nanowires
The wires mimic 1-D structures of biological neurons: axons and dendrites.
Memristive coating forms artificial synapses at interface with silicon neurons.
OUR AGENDA

## Slide 5
But what plays the mischief with this masterly.
Memristive Nanowire Neural Network (MN3)
Excellent scaling characteristics: ~ 1 billion trainable parameters per cm2 [1].
Intrinsic small-world connectivity [1].
Supports both reservoir computing [2] and deep learning [3] algorithms.
[1] R. Pantone, J. Kendall, and J. Nino, “Memristive Nanowires Exhibit Small-World Connectivity,” Neural Networks (in press).
[2] L. Suarez, J. Kendall, and J. Nino, “Evaluation of the Computational Capabilities of a Memristive Random Network (MN3) under the context of Reservoir Computing Mathematical and Computational Analysis,” Neural Networks (in press).
[3] J. Kendall and J. Nino, Deep Learning in Bipartite Memristive Networks. U.S. Patent Application No. 15/985,212. Unpublished (filing date 05/21/2018).

## Slide 6
MN3 Proof of Concept
100 electrode ball-grid array.
22 μm diameter tungsten wires (W).
Wires oxidized at 400 °C to form a memristive coating tungsten oxide (WOx).

## Slide 7
MN3 Hardware Details
Single W-WOx Wire
A thin layer of tungsten oxide is thermally grown on the 22 μm diameter wires.
MN3 with Ag Electrodes
Wires are randomly deposited on an electrode array and connected to the array using silver paste.
W/WOx/Ag I-V Curve
Resulting I-V curves for the tungsten wires with Ag top electrode.

## Slide 8
But what plays the mischief with this masterly.
Analog Spiking Neurons
Axon Hillock model (Mead 1989).
Built and tested with discrete components.
Coupled with MN3 memristor network through single-transistor synapses.

## Slide 9
OUR AGENDA
MN3-Based Liquid State Machine
Custom designed PCB with 40 axon-hillock spiking neurons.
10 input neurons with variable tuning curves.
Teensy 3.6 microcontroller and Altera FPGA for I/O and spike detection.

## Slide 10
Liquid State Machine System Overview

## Slide 11
Liquid State Machine
Results
Mackey-Glass Predictions
Actual Data: Green Curve
Prediction: Blue Curve (overlaid)
Spoken Digits Spike Raster
Achieves 94% accuracy on an isolated subset of the TIDIGITS spoken digits dataset.

## Slide 12
But what plays the mischief with this masterly.
Next Steps and Future Work
Successfully trained deep MN3 models via novel backpropagation algorithm.
Sparse Vector-Matrix Multiply (VMM) A.I. Accelerator.
First 5,000 neuron VLSI chip planned for 2019 (TSMC 180 nm).